GEO-FIX® USPs

ORIGINAL

- Cost effective – bigger tubs, more for your money.

- Vacuum packed in extra strong 128 micron sealed foils for freshness. Removes oxygen, bacteria and preserves shelf life.

- Superior strength to competitors – flexural and compressive.

- Great export product for dry climates, (cold or warm).

- Indoor or outdoor use.

- Can be used in temperatures below freezing.

- Rapid setting, fast drying.

- None staining if residue swept away.

- Fastest curing product on the market – 2 1/2 hours at 200C – (competitors typically 6 – 12 hours – up to several days!).

- Proven Track record – Original polymeric jointing sand - 25 years use in market.

- Freeze thaw exceeds BCRL:BM2:1993 – exceeds 100 cycles.

- Non staining – no need to use water to protect the paving from polymer staining.

- A permeable bed is not required as long as suitable falls are incorporated into the sub-base to allow water to drain away

- Long lasting and durable.

- Size: 20Kg.

- Colours: buff and grey.

ALL WEATHER

- Vacuum packed in extra strong 128 micron sealed foils for freshness. Removes oxygen, bacteria and preserves shelf life.

- A Hydrophobic product which totally repels water.

- Fast Curing time when allowed to dry 4 – 12 hours.

- Colour fast sands to produce consistent colour. No pigments used.

- Minimum depth 15mm which suits most types of concrete, ceramic, porcelain and natural stone paving, (other products min 20-25mm).

- When laying porcelain tiles, that are generally a minimum thickness of 20mm, migration of the mortar bed and base slurry coat will impact on the joint depth and often lead to jointing compounds popping out as they require a full 20mm clearance. Geo-Fix, All Weather has been designed for use in joints down to 15mm deep, therefore will not be compromised in this situation.

- Geo-Fix Track Record.

- Freeze Thaw DD/CEN/TS 772:22:2006 exceeds 100 cycles representing the most severe conditions which the product was likely to be subjected to.

- Works in all weather conditions – making this a product that can be used 365 days of the year.

- A permeable bed is not required as long as suitable falls are incorporated into the sub-base to allow water to drain away

- Long lasting and durable.

- Size: 14Kg.

- Colours: Anthracite, graphite, stone, mid grey, slate grey and buff.